APPENDICES

APPENDIX A Experimental data for C8 adsorption study on carbon black.

Weight of carbon black		=  2.5 g

Volume of solution		=  20 ml

Temperature			=  30(C

pH				=  9

Table A1  Data for C8 adsorption on carbon black without calcium addition.

| Initial C8 | Equilibrium C8 | Different C8 | C8 adsorption |
| --- | --- | --- | --- |
| concentration | Concentration | concentration | (mole/m2) |
| (M) | (M) | (M) |  |
| 1925.00 | 1689.20 | 235.80 | 0.0246 |
| 2891.67 | 2353.95 | 537.72 | 0.0560 |
| 3863.02 | 2905.25 | 957.77 | 0.0998 |
| 7729.17 | 5653.09 | 2076.07 | 0.2163 |
| 8682.29 | 5923.05 | 2759.24 | 0.2874 |
| 10244.79 | 7337.93 | 2906.86 | 0.3028 |
| 19942.71 | 14979.51 | 4963.20 | 0.5170 |
| 37619.79 | 28366.43 | 9253.36 | 0.9639 |
| 49619.79 | 37626.48 | 11993.32 | 1.2493 |
| 61666.67 | 50286.02 | 11380.64 | 1.1855 |
| 69114.58 | 55400.90 | 13713.68 | 1.4285 |
| 78229.17 | 62775.32 | 15453.85 | 1.6098 |
| 87604.17 | 72211.67 | 15392.50 | 1.6034 |
| 97395.83 | 80397.84 | 16997.99 | 1.7706 |
| 117031.25 | 99700.15 | 17331.10 | 1.8053 |
| 136718.75 | 112481.02 | 24237.73 | 2.5248 |
| 175156.25 | 151189.39 | 23966.86 | 2.4965 |
| 198177.08 | 168659.69 | 29517.40 | 3.0747 |
| 248203.13 | 219970.99 | 28232.13 | 2.9408 |
| 299739.58 | 254677.87 | 45061.71 | 4.6939 |
| 385937.50 | 355063.22 | 30874.28 | 3.2161 |
| 593229.17 | 524894.98 | 68334.18 | 7.1181 |
| 682812.50 | 621255.33 | 61557.17 | 6.4122 |

Table A2  Data for C8 adsorption on carbon black at the initial calcium concentration 100

| Initial C8 | Equilibrium C8 | Different C8 | C8 adsorption |
| --- | --- | --- | --- |
| concentration | concentration | concentration | (mole/m2) |
| (M) | (M) | (M) |  |
| 961.04 | 746.02 | 215.02 | 0.0224 |
| 1912.50 | 1419.32 | 493.18 | 0.0514 |
| 2854.17 | 1971.09 | 883.07 | 0.0920 |
| 3918.75 | 2975.23 | 943.52 | 0.0983 |
| 4824.48 | 3211.66 | 1612.82 | 0.1680 |
| 5614.58 | 3849.47 | 1765.11 | 0.1839 |
| 6687.50 | 5023.20 | 1664.30 | 0.1734 |
| 7651.04 | 5723.08 | 1927.96 | 0.2008 |
| 8546.88 | 6103.03 | 2443.84 | 0.2546 |
| 9546.88 | 6687.97 | 2858.90 | 0.2978 |
| 20171.88 | 16410.23 | 3761.65 | 0.3918 |
| 29661.46 | 22414.69 | 7246.76 | 0.7549 |
| 39416.67 | 31270.55 | 8146.12 | 0.8486 |
| 48088.54 | 37145.56 | 10942.98 | 1.1399 |
| 58541.67 | 47242.98 | 11298.69 | 1.1769 |
| 67760.42 | 54197.25 | 13563.17 | 1.4128 |
| 77291.67 | 61621.26 | 15670.40 | 1.6323 |
| 87447.92 | 68797.85 | 18650.06 | 1.9427 |
| 97552.08 | 77132.90 | 20419.19 | 2.1270 |
| 113593.75 | 91654.61 | 21939.14 | 2.2853 |
| 134895.83 | 106995.03 | 27900.80 | 2.9063 |
| 158177.08 | 129051.37 | 29125.72 | 3.0339 |
| 177239.58 | 147077.11 | 30162.47 | 3.1419 |
| 198958.33 | 166159.13 | 32799.20 | 3.4166 |

Table A3  Data for C8 adsorption on carbon black at the initial calcium concentration 700

| Initial C8 | Equilibrium C8 | Different C8 | C8 adsorption |
| --- | --- | --- | --- |
| concentration | concentration | concentration | (mole/m2) |
| (M) | (M) | (M) |  |
| 944.79 | 300.54 | 644.26 | 0.0671 |
| 1838.54 | 711.54 | 1127.01 | 0.1174 |
| 2832.29 | 1365.34 | 1466.95 | 0.1528 |
| 5526.04 | 3630.53 | 1895.51 | 0.1974 |
| 7541.67 | 5203.17 | 2338.50 | 0.2436 |
| 9380.21 | 6313.01 | 3067.20 | 0.3195 |
| 12281.25 | 7472.92 | 4808.33 | 0.5009 |
| 16130.21 | 10483.12 | 5647.09 | 0.5882 |
| 20541.67 | 14774.42 | 5767.25 | 0.6008 |
| 29765.63 | 22459.74 | 7305.89 | 0.7610 |
| 38848.96 | 30309.13 | 8539.83 | 0.8896 |

Table A4  Data for C8 adsorption on carbon black at the initial calcium concentration 1000.

| Initial C8 | Equilibrium C8 | Different C8 | C8 adsorption |
| --- | --- | --- | --- |
| concentration | concentration | concentration | (mole/m2) |
| (M) | (M) | (M) |  |
| 1958.33 | 676.02 | 1282.31 | 0.1336 |
| 4092.19 | 1946.71 | 2145.47 | 0.2235 |
| 4968.23 | 2458.14 | 2510.09 | 0.2615 |
| 5796.88 | 2875.98 | 2920.90 | 0.3043 |
| 12567.71 | 6685.84 | 5881.87 | 0.6127 |
| 16854.17 | 9825.31 | 7028.86 | 0.7322 |
| 19958.33 | 11959.89 | 7998.45 | 0.8332 |
| 29895.83 | 20889.68 | 9006.15 | 0.9381 |

Table A5  Data for the amount of adsorbed calcium on carbon black from C8 adsorption study at the initial calcium concentration 100 

| Initial C8 | Equilibrium C8 | Equilibrium calcium | Calcium |
| --- | --- | --- | --- |
| concentration | concentration | concentration | adsorption |
| (M) | (M) | (M) | (mole/m2) |
| 0 | 0 | 96.25 | 0.0004 |
| 961.04 | 746.02 | 51.25 | 0.0051 |
| 1912.50 | 1419.32 | 27.50 | 0.0076 |
| 2854.17 | 1971.09 | 26.25 | 0.0077 |
| 3918.75 | 2975.23 | 23.75 | 0.0079 |
| 4824.48 | 3211.66 | 27.50 | 0.0076 |
| 5614.58 | 3849.47 | 26.25 | 0.0077 |
| 6687.50 | 5023.20 | 43.75 | 0.0059 |
| 7651.04 | 5723.08 | 26.25 | 0.0077 |
| 8546.88 | 6103.03 | 25.00 | 0.0078 |
| 9546.88 | 6687.97 | 23.75 | 0.0079 |
| 20171.88 | 16410.23 | 23.75 | 0.0079 |
| 29661.46 | 22414.69 | 18.75 | 0.0085 |
| 39416.67 | 31270.55 | 21.25 | 0.0082 |
| 48088.54 | 37145.56 | 20.00 | 0.0083 |
| 58541.67 | 47242.98 | 18.75 | 0.0085 |
| 67760.42 | 54197.25 | 17.50 | 0.0086 |
| 77291.67 | 61621.26 | 15.00 | 0.0089 |
| 87447.92 | 68797.85 | 16.25 | 0.0087 |
| 97552.08 | 77132.90 | 15.00 | 0.0089 |
| 113593.75 | 91654.61 | 15.00 | 0.0089 |
| 134895.83 | 106995.03 | 12.50 | 0.0091 |
| 158177.08 | 129051.37 | 11.25 | 0.0092 |
| 177239.58 | 147077.11 | 11.25 | 0.0092 |
| 198958.33 | 166159.13 | 11.25 | 0.0092 |

Table A6  Data for the amount of adsorbed calcium on carbon black from C8 adsorption study at the initial calcium concentration 700 

| Initial C8 | Equilibrium C8 | Equilibrium calcium | Calcium |
| --- | --- | --- | --- |
| concentration | concentration | concentration | Adsorption |
| (M) | (M) | (M) | (mole/m2) |
| 0 | 0 | 463.50 | 0.0338 |
| 944.79 | 300.54 | 32.50 | 0.0787 |
| 1838.54 | 711.54 | 23.25 | 0.0797 |
| 2832.29 | 1365.34 | 22.75 | 0.0797 |
| 5526.04 | 3630.53 | 42.25 | 0.0777 |
| 7541.67 | 5203.17 | 22.00 | 0.0798 |
| 9380.21 | 6313.01 | 43.00 | 0.0776 |
| 12281.25 | 7472.92 | 20.00 | 0.0800 |
| 16130.21 | 10483.12 | 21.50 | 0.0798 |
| 20541.67 | 14774.42 | 20.25 | 0.0800 |
| 29765.63 | 22459.74 | 26.25 | 0.0793 |
| 38848.96 | 30309.13 | 20.25 | 0.0800 |

Table A7  Data for the amount of adsorbed calcium on carbon black from C8 adsorption study at the initial calcium concentration 1000 

| Initial C8 | Equilibrium C8 | Equilibrium calcium | Calcium |
| --- | --- | --- | --- |
| concentration | concentration | concentration | Adsorption |
| (M) | (M) | (M) | (mole/m2) |
| 0 | 0 | 53.13 | 0.0986 |
| 1958.33 | 676.02 | 34.50 | 0.1006 |
| 4092.19 | 1946.71 | 33.25 | 0.1007 |
| 4968.23 | 2458.14 | 34.75 | 0.1005 |
| 5796.88 | 2875.98 | 57.75 | 0.0982 |
| 12567.71 | 6685.84 | 83.00 | 0.0955 |
| 16854.17 | 9825.31 | 58.25 | 0.0981 |
| 19958.33 | 11959.89 | 52.25 | 0.0987 |
| 29895.83 | 20889.68 | 31.50 | 0.1009 |

APPENDIX B

Experimental data for C8 adsorption study on paper fiber.

Weight of dry paper fiber	=  1.0 g

Volume of solution		=  25 ml

Temperature			=  30(C

pH				=  9

Table B1  Data for C8 adsorption on paper fiber without calcium addition.

| Initial C8 | Equilibrium C8 | Different C8 | Adsorption |
| --- | --- | --- | --- |
| concentration | concentration | concentration | (mole/m2) |
| (M) | (M) | (M) |  |
| 571.56 | 128.13 | 443.44 | 0.1109 |
| 2043.75 | 1462.50 | 581.25 | 0.1453 |
| 3081.25 | 2470.83 | 610.42 | 0.1526 |
| 4064.58 | 3603.13 | 461.46 | 0.1154 |
| 5126.04 | 4366.67 | 759.38 | 0.1898 |
| 6682.29 | 5755.21 | 927.08 | 0.2318 |
| 8760.42 | 7668.75 | 1091.67 | 0.2729 |
| 10217.71 | 9242.71 | 975.00 | 0.2438 |
| 17942.71 | 16008.33 | 1934.38 | 0.4836 |
| 21369.79 | 19273.96 | 2095.83 | 0.5240 |
| 31614.58 | 29081.25 | 2533.33 | 0.6333 |
| 42343.75 | 39055.21 | 3288.54 | 0.8221 |
| 61119.79 | 54263.54 | 6856.25 | 1.7141 |
| 81093.75 | 72362.50 | 8731.25 | 2.1828 |
| 97812.50 | 90826.04 | 6986.46 | 1.7466 |
| 118489.58 | 107753.13 | 10736.46 | 2.6841 |
| 155963.54 | 144367.71 | 11595.83 | 2.8990 |
| 195104.17 | 183013.54 | 12090.63 | 3.0227 |
| 295104.17 | 279576.04 | 15528.12 | 3.8820 |
| 388593.75 | 364419.79 | 24173.96 | 6.0435 |
| 476093.75 | 443326.04 | 32767.71 | 8.1919 |
| 568750.00 | 536242.71 | 32507.29 | 8.1268 |
| 684895.83 | 653638.54 | 31257.29 | 7.8143 |
| 775937.50 | 744471.88 | 31465.63 | 7.8664 |

Table B2  Data for C8 adsorption on paper fiber at the initial calcium concentration 1000

| Initial C8 | Equilibrium C8 | Different C8 | Adsorption |
| --- | --- | --- | --- |
| concentration | concentration | concentration | (mole/m2) |
| (M) | (M) | (M) |  |
| 1060.42 | 257.29 | 803.13 | 0.2008 |
| 2043.75 | 1192.71 | 851.04 | 0.2128 |
| 4022.92 | 2884.38 | 1138.54 | 0.2846 |
| 6029.17 | 5061.46 | 967.71 | 0.2419 |
| 7898.96 | 6827.08 | 1071.88 | 0.2680 |
| 9876.04 | 8807.29 | 1068.75 | 0.2672 |
| 15437.50 | 13817.71 | 1619.79 | 0.4049 |
| 20281.25 | 18130.21 | 2151.04 | 0.5378 |
| 24510.42 | 21755.21 | 2755.21 | 0.6888 |
| 30604.17 | 26796.88 | 3807.29 | 0.9518 |
| 34135.42 | 30630.21 | 3505.21 | 0.8763 |

Table B3  Data for C8 adsorption on paper fiber at the initial calcium concentration 2000

| Initial C8 | Equilibrium C8 | Different C8 | Adsorption |
| --- | --- | --- | --- |
| concentration | concentration | concentration | (mole/m2) |
| (M) | (M) | (M) |  |
| 1079.17 | 419.79 | 659.38 | 0.1648 |
| 2054.17 | 1358.33 | 695.83 | 0.1740 |
| 3072.92 | 2370.83 | 702.08 | 0.1755 |
| 4084.38 | 3257.29 | 827.08 | 0.2068 |
| 6007.29 | 4872.92 | 1134.38 | 0.2836 |
| 7878.13 | 7035.42 | 842.71 | 0.2107 |
| 9917.71 | 8723.96 | 1193.75 | 0.2984 |

Table B4  Data for the amount of adsorbed calcium on paper fiber from C8 adsorption study at the initial calcium concentration 1000 

| Initial C8 | Equilibrium C8 | Equilibrium calcium | Calcium |
| --- | --- | --- | --- |
| concentration | concentration | concentration | adsorption |
| (M) | (M) | (M) | (mole/m2) |
| 0 | 0 | 648.1250 | 0.0919 |
| 1060.42 | 257.29 | 711.2500 | 0.0761 |
| 2043.75 | 1192.71 | 746.8750 | 0.0672 |
| 4022.92 | 2884.38 | 751.2500 | 0.0661 |
| 6029.17 | 5061.46 | 790.6250 | 0.0563 |
| 7898.96 | 6827.08 | 795.6250 | 0.0550 |
| 9876.04 | 8807.29 | 803.7500 | 0.0530 |
| 15437.50 | 13817.71 | 801.2500 | 0.0536 |
| 20281.25 | 18130.21 | 900.6250 | 0.0288 |
| 24510.42 | 21755.21 | 956.2500 | 0.0148 |
| 30604.17 | 26796.88 | 965.0000 | 0.0127 |
| 34135.42 | 30630.21 | 963.1250 | 0.0131 |

Table B5  Data for the amount of adsorbed calcium on paper fiber from C8 adsorption study at the initial calcium concentration 2000 

| Initial C8 | Equilibrium C8 | Equilibrium calcium | Calcium |
| --- | --- | --- | --- |
| concentration | concentration | concentration | adsorption |
| (M) | (M) | (M) | (mole/m2) |
| 0 | 0 | 1606.8750 | 0.1405 |
| 1079.17 | 419.79 | 1775.6250 | 0.0983 |
| 2054.17 | 1358.33 | 1808.1250 | 0.0902 |
| 3072.92 | 2370.83 | 1810.6250 | 0.0895 |
| 4084.38 | 3257.29 | 1840.6250 | 0.0820 |
| 6007.29 | 4872.92 | 1843.1250 | 0.0814 |
| 7878.13 | 7035.42 | 1823.1250 | 0.0864 |
| 9917.71 | 8723.96 | 1854.3750 | 0.0786 |

APPENDIX C

Experimental data for calcium adsorption on carbon black.

Weight of carbon black		=  2.5 g

Volume of solution		=  20 ml

Temperature			=  30(C

pH				=  9

Table C1  Data for calcium adsorption on carbon black without C8 addition.

| Initial calcium | Final calcium | Different calcium | Adsorption |
| --- | --- | --- | --- |
| concentration | concentration | concentration | (mole/m2) |
| (M) | (M) | (M) |  |
| 1027.50 | 53.13 | 974.38 | 0.1015 |
| 1268.13 | 76.88 | 1191.25 | 0.1241 |
| 1523.75 | 46.88 | 1476.88 | 0.1538 |
| 2293.75 | 468.75 | 1825.00 | 0.1901 |
| 4100.00 | 1175.00 | 2925.00 | 0.3047 |
| 5800.00 | 1737.50 | 4062.50 | 0.4232 |
| 7287.50 | 2850.00 | 4437.50 | 0.4622 |
| 9337.50 | 4175.00 | 5162.50 | 0.5378 |
| 11300.00 | 5093.75 | 6206.25 | 0.6465 |
| 12925.00 | 6593.75 | 6331.25 | 0.6595 |
| 15400.00 | 7800.00 | 7600.00 | 0.7917 |
| 16443.75 | 9262.50 | 7181.25 | 0.7480 |
| 19337.50 | 11812.50 | 7525.00 | 0.7839 |
| 21637.50 | 13912.50 | 7725.00 | 0.8047 |
| 23537.50 | 15768.75 | 7768.75 | 0.8092 |
| 26662.50 | 18550.00 | 8112.50 | 0.8451 |
| 28675.00 | 20237.50 | 8437.50 | 0.8789 |
| 30687.50 | 22360.00 | 8327.50 | 0.8674 |
| 32712.50 | 24062.50 | 8650.00 | 0.9010 |
| 34687.50 | 26262.50 | 8425.00 | 0.8776 |

Table C2  Data for calcium adsorption on carbon black at the initial C8 concentration 100

| Initial calcium | Final calcium | Different calcium | Adsorption |
| --- | --- | --- | --- |
| concentration | concentration | concentration | (mole/m2) |
| (M) | (M) | (M) |  |
| 638.75 | 81.25 | 557.50 | 0.0581 |
| 1192.19 | 51.88 | 1140.31 | 0.1188 |
| 2681.25 | 506.25 | 2175.00 | 0.2266 |
| 4656.25 | 687.50 | 3968.75 | 0.4134 |
| 6468.75 | 2475.00 | 3993.75 | 0.4160 |
| 8525.00 | 2962.50 | 5562.50 | 0.5794 |
| 10350.00 | 4900.00 | 5450.00 | 0.5677 |
| 14862.50 | 8206.25 | 6656.25 | 0.6934 |
| 19368.75 | 12300.00 | 7068.75 | 0.7363 |
| 23562.50 | 15575.00 | 7987.50 | 0.8320 |
| 27625.00 | 19325.00 | 8300.00 | 0.8646 |
| 31687.50 | 22837.50 | 8850.00 | 0.9219 |
| 35587.50 | 26937.50 | 8650.00 | 0.9010 |

Table C3  Data for calcium adsorption on carbon black at the initial C8 concentration 500.

| Initial calcium | Final calcium | Different calcium | Adsorption |
| --- | --- | --- | --- |
| concentration | concentration | concentration | (mole/m2) |
| (M) | (M) | (M) |  |
| 571.88 | 105.00 | 466.88 | 0.0486 |
| 1026.25 | 93.75 | 932.50 | 0.0971 |
| 2068.75 | 150.00 | 1918.75 | 0.1999 |
| 4500.00 | 1143.75 | 3356.25 | 0.3496 |
| 6031.25 | 1337.50 | 4693.75 | 0.4889 |
| 8443.75 | 2381.25 | 6062.50 | 0.6315 |
| 10275.00 | 3468.75 | 6806.25 | 0.7090 |
| 15143.75 | 6987.50 | 8156.25 | 0.8496 |
| 18568.75 | 9500.00 | 9068.75 | 0.9447 |
| 22487.50 | 12812.50 | 9675.00 | 1.0078 |
| 26475.00 | 16887.50 | 9587.50 | 0.9987 |
| 30700.00 | 20712.50 | 9987.50 | 1.0404 |
| 34300.00 | 24700.00 | 9600.00 | 1.0000 |

Table C4  Data for calcium adsorption on carbon black at the initial C8 concentration 1000.

| Initial calcium | Final calcium | Different calcium | Adsorption |
| --- | --- | --- | --- |
| concentration | concentration | concentration | (mole/m2) |
| (M) | (M) | (M) |  |
| 540.00 | 93.75 | 446.25 | 0.0465 |
| 1039.38 | 88.13 | 951.25 | 0.0991 |
| 2062.50 | 175.00 | 1887.50 | 0.1966 |
| 4212.50 | 618.75 | 3593.75 | 0.3743 |
| 5981.25 | 1362.50 | 4618.75 | 0.4811 |
| 7900.00 | 1712.50 | 6187.50 | 0.6445 |
| 10056.25 | 3012.50 | 7043.75 | 0.7337 |
| 14487.50 | 5675.00 | 8812.50 | 0.9180 |
| 18506.25 | 8937.50 | 9568.75 | 0.9967 |
| 22175.00 | 12162.50 | 10012.50 | 1.0430 |
| 26462.50 | 16237.50 | 10225.00 | 1.0651 |
| 30075.00 | 19687.50 | 10387.50 | 1.0820 |
| 34800.00 | 24600.00 | 10200.00 | 1.0625 |

Table C5  Data for the amount of adsorbed C8 on carbon black from calcium adsorption study at the initial C8 concentration 500 

| Initial calcium | Equilibrium calcium | Equilibrium C8 | C8 adsorption |
| --- | --- | --- | --- |
| concentration | concentration | concentration | (mole/m2) |
| (M) | (M) | (M) |  |
| 2068.75 | 150.00 | 423.96 | 0.0079 |
| 8443.75 | 2381.25 | 289.38 | 0.0219 |
| 10275.00 | 3468.75 | 220.42 | 0.0291 |
| 15143.75 | 6987.50 | 167.60 | 0.0346 |
| 18568.75 | 9500.00 | 154.79 | 0.0360 |
| 22487.50 | 12812.50 | 126.77 | 0.0389 |
| 26475.00 | 16887.50 | 168.23 | 0.0346 |
| 30700.00 | 20712.50 | 126.56 | 0.0389 |
| 34300.00 | 24700.00 | 130.00 | 0.0385 |

Table C6  Data for the amount of adsorbed C8 on carbon black from calcium adsorption study at the initial C8 concentration 1000 

| Initial calcium | Equilibrium calcium | Equilibrium C8 | C8 adsorption |
| --- | --- | --- | --- |
| concentration | concentration | concentration | (mole/m2) |
| (M) | (M) | (M) |  |
| 540.00 | 93.75 | 814.27 | 0.0180 |
| 4212.50 | 618.75 | 697.29 | 0.0302 |
| 5981.25 | 1362.50 | 428.33 | 0.0582 |
| 7900.00 | 1712.50 | 413.75 | 0.0598 |
| 10056.25 | 3012.50 | 308.85 | 0.0707 |
| 14487.50 | 5675.00 | 249.90 | 0.0768 |
| 18506.25 | 8937.50 | 220.10 | 0.0799 |
| 22175.00 | 12162.50 | 186.88 | 0.0834 |
| 26462.50 | 16237.50 | 200.94 | 0.0819 |
| 30075.00 | 19687.50 | 201.46 | 0.0819 |
| 34800.00 | 24600.00 | 167.40 | 0.0854 |

APPENDIX D

Experimental data for calcium adsorption on paper fiber.

Weight of dry paper fiber	=  1.0 g

Volume of solution		=  25 ml

Temperature			=  30(C

pH				=  9

Table D1  Data for calcium adsorption on paper fiber without C8 addition.

| Initial calcium | Equilibrium calcium | Different calcium | Adsorption |
| --- | --- | --- | --- |
| concentration | concentration | concentration | (mole/m2) |
| (M) | (M) | (M) |  |
| 565.00 | 224.38 | 340.63 | 0.0852 |
| 1079.38 | 590.00 | 489.38 | 0.1223 |
| 2793.75 | 1446.88 | 1346.88 | 0.3367 |
| 4925.00 | 3889.38 | 3478.13 | 0.8695 |
| 9018.75 | 6551.88 | 2466.88 | 0.6167 |
| 13056.25 | 9595.63 | 3460.63 | 0.8652 |
| 17925.00 | 12339.38 | 5585.63 | 1.3964 |
| 22350.00 | 15576.88 | 6773.13 | 1.6933 |
| 26987.50 | 19564.38 | 7423.13 | 1.8558 |
| 33937.50 | 24889.38 | 9048.13 | 2.2620 |
| 43462.50 | 35514.38 | 7948.13 | 1.9870 |

Table D2  Data for calcium adsorption on paper fiber at the initial C8 concentration 500

| Initial calcium | Equilibrium calcium | Different calcium | Adsorption |
| --- | --- | --- | --- |
| concentration | concentration | concentration | (mole/m2) |
| (M) | (M) | (M) |  |
| 980.00 | 430.00 | 550.00 | 0.1375 |
| 2806.25 | 1192.50 | 1613.75 | 0.4034 |
| 4518.75 | 2797.50 | 1721.25 | 0.4303 |
| 8643.75 | 6053.75 | 2590.00 | 0.6475 |
| 12331.25 | 9728.75 | 2602.50 | 0.6506 |
| 17737.50 | 14066.25 | 3671.25 | 0.9178 |
| 21087.50 | 16141.25 | 4946.25 | 1.2366 |
| 30137.50 | 24741.25 | 5396.25 | 1.3491 |
| 40675.00 | 34478.75 | 6196.25 | 1.5491 |

Table D3  Data for calcium adsorption on paper fiber at the initial C8 concentration 1000

| Initial calcium | Equilibrium calcium | Different calcium | Adsorption |
| --- | --- | --- | --- |
| concentration | concentration | concentration | (mole/m2) |
| (M) | (M) | (M) |  |
| 1136.25 | 468.13 | 668.13 | 0.1670 |
| 2406.25 | 1071.88 | 1334.38 | 0.3336 |
| 4100.00 | 2269.38 | 1830.63 | 0.4577 |
| 8262.50 | 6056.88 | 2205.63 | 0.5514 |
| 12775.00 | 10281.88 | 2493.13 | 0.6233 |
| 15881.25 | 12738.13 | 3143.13 | 0.7858 |
| 20425.00 | 16600.63 | 3824.38 | 0.9561 |
| 40612.50 | 37238.13 | 3374.38 | 0.8436 |

Table D4  Data for the amount of adsorbed C8 on paper fiber from calcium adsorption study at the initial C8 concentration 500 

| Initial calcium | Equilibrium calcium | Equilibrium C8 | C8 adsorption |
| --- | --- | --- | --- |
| concentration | concentration | concentration | (mole/m2) |
| (M) | (M) | (M) |  |
| 980.00 | 430.00 | 54.17 | 0.0464 |
| 2806.25 | 1192.50 | 93.75 | 0.0423 |
| 4518.75 | 2797.50 | 180.21 | 0.0333 |
| 8643.75 | 6053.75 | 223.96 | 0.0288 |
| 12331.25 | 9728.75 | 235.42 | 0.0276 |
| 17737.50 | 14066.25 | 275.00 | 0.0234 |
| 21087.50 | 16141.25 | 411.46 | 0.0092 |
| 30137.50 | 24741.25 | 437.50 | 0.0065 |

Table D5  Data for the amount of adsorbed C8 on paper fiber from calcium adsorption study at the initial C8 concentration 1000 

| Initial calcium | Equilibrium calcium | Equilibrium C8 | C8 adsorption |
| --- | --- | --- | --- |
| concentration | concentration | concentration | (mole/m2) |
| (M) | (M) | (M) |  |
| 1136.25 | 468.13 | 668.75 | 0.0557 |
| 2406.25 | 1071.88 | 797.92 | 0.0422 |
| 4100.00 | 2269.38 | 813.54 | 0.0406 |
| 8262.50 | 6056.88 | 836.46 | 0.0382 |
| 12775.00 | 10281.88 | 892.71 | 0.0323 |
| 15881.25 | 12738.13 | 931.25 | 0.0283 |
| 20425.00 | 16600.63 | 1042.71 | 0.0167 |
| 40612.50 | 37238.13 | 1046.88 | 0.0163 |

## APPENDIX E

## Experimental data for zeta potential of carbon black.

Weight of carbon black		=  1.5 mg

Volume of solution		=  40 ml

Temperature			=  30(C

pH				=  9

Table E1  Data for zeta potential of carbon black with varying C8 concentration and  without calcium addition.

| C8 Concentration (M) | 651.46 | 1179.17 | 2377.08 | 3566.67 | 4732.29 | 7296.88 |
| --- | --- | --- | --- | --- | --- | --- |
| (-) Zeta potential (mV) | 1 | 42.4 | 42.7 | 39.7 | 39.7 | 39.6 | 37.5 |
|  | 2 | 42.6 | 44.0 | 40.0 | 43.4 | 39.3 | 37.9 |
|  | 3 | 44.8 | 40.5 | 41.9 | 38.2 | 41.3 | 39.4 |
|  | 4 | 45.6 | 42.1 | 38.8 | 40.6 | 40.3 | 38.5 |
|  | 5 | 45.9 | 42.6 | 40.1 | 41.7 | 41.9 | 37.2 |
|  | 6 | 42.1 | 41.9 | 38.7 | 39.1 | 40.4 | 41.1 |
|  | 7 | 42.0 | 41.8 | 41.1 | 42.4 | 38.9 | 38.0 |
|  | 8 | 44.1 | 44.7 | 39.0 | 40.4 | 38.6 | 40.4 |
|  | 9 | 44.0 | 41.2 | 41.9 | 40.0 | 41.4 | 38.9 |
|  | 10 | 39.7 | 42.7 | 38.6 | 39.1 | 38.5 | 37.4 |
|  | 11 | 42.2 | 41.4 | 40.3 | 38.9 | 40.4 | 39.9 |
|  | 12 | 43.5 | 40.5 | 38.9 | 38.5 | 41.4 | 40.5 |
| Average zeta potential (mV) |  | 43.2 | 42.2 | 39.9 | 40.2 | 40.2 | 38.9 |
| Standard deviation | 1.68 | 1.22 | 1.15 | 1.55 | 1.13 | 1.29 |

Table E2  Data for zeta potential of carbon black with varying C8 concentration and the initial calcium concentration 100     M.

| C8 Concentration (M) | 557.81 | 1134.38 | 2212.50 | 3356.25 | 4451.04 | 6329.17 | 12437.50 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| (-) Zeta potential (mV) | 1 | 36.2 | 34.4 | 36.2 | 33.7 | 28.3 | 33.3 | 32.4 |
|  | 2 | 37.9 | 35.9 | 36.1 | 32.7 | 31.7 | 28.5 | 31.5 |
|  | 3 | 35.8 | 37.5 | 34.6 | 34.7 | 30.5 | 29.1 | 29.5 |
|  | 4 | 36.2 | 38.3 | 36.7 | 35.0 | 30.0 | 30.3 | 29.1 |
|  | 5 | 33.6 | 33.3 | 34.9 | 34.6 | 30.0 | 29.6 | 32.5 |
|  | 6 | 36.3 | 37.4 | 33.7 | 32.7 | 31.9 | 31.2 | 30.0 |
|  | 7 | 38.7 | 37.7 | 35.1 | 33.4 | 32.4 | 32.1 | 29.1 |
|  | 8 | 37.7 | 36.5 | 34.8 | 38.4 | 28.9 | 31.6 | 28.4 |
|  | 9 | 35.5 | 36.9 | 39.2 | 35.4 | 28.0 | 33.1 | 28.2 |
|  | 10 | 37.6 | 36.5 | 33.7 | 34.7 | 31.9 | 30.4 | 31.8 |
|  | 11 | 38.7 | 34.4 | 33.9 | 32.6 | 32.3 | 30.4 | 29.8 |
|  | 12 | 39.3 | 36.3 | 32.8 | 36.9 | 31.5 | 29.4 | 29.5 |
| Average zeta potential (mV) |  | 37.0 | 36.3 | 35.1 | 34.6 | 30.6 | 30.8 | 30.2 |
| Standard deviation | 1.57 | 1.46 | 1.65 | 1.68 | 1.51 | 1.48 | 1.45 |

Table E3  Data for zeta potential of carbon black with varying C8 concentration and the initial calcium concentration 700     M.

| C8 Concentration (M) | 644.90 | 1190.63 | 2380.21 | 3577.08 | 4779.17 | 8177.08 | 14114.58 | 17302.08 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (-) Zeta potential (mV) | 1 | 28.0 | 27.6 | 29.4 | 26.1 | 25.0 | 21.0 | 20.2 | 20.5 |
|  | 2 | 29.3 | 29.8 | 28.6 | 23.1 | 20.3 | 25.0 | 22.6 | 19.2 |
|  | 3 | 31.8 | 30.9 | 30.6 | 25.3 | 23.7 | 22.5 | 21.8 | 19.9 |
|  | 4 | 30.0 | 28.3 | 28.0 | 25.0 | 23.9 | 25.0 | 20.9 | 21.2 |
|  | 5 | 32.8 | 27.7 | 26.2 | 23.6 | 21.6 | 23.2 | 21.4 | 20.0 |
|  | 6 | 32.2 | 27.3 | 30.7 | 23.9 | 23.0 | 22.6 | 23.6 | 18.6 |
|  | 7 | 30.0 | 30.2 | 28.8 | 24.5 | 21.2 | 23.0 | 20.7 | 21.5 |
|  | 8 | 30.9 | 30.9 | 28.3 | 25.0 | 20.6 | 22.1 | 20.0 | 20.9 |
|  | 9 | 31.4 | 29.1 | 26.0 | 27.1 | 23.2 | 26.0 | 21.9 | 22.7 |
|  | 10 | 31.9 | 28.8 | 31.2 | 25.9 | 21.5 | 21.0 | 20.2 | 20.4 |
|  | 11 | 30.4 | 27.1 | 28.6 | 26.2 | 24.4 | 22.5 | 19.6 | 21.6 |
|  | 12 | 28.8 | 26.8 | 29.9 | 25.8 | 21.8 | 21.6 | 21.0 | 23.5 |
| Average zeta potential (mV) |  | 30.6 | 28.7 | 28.9 | 25.1 | 22.5 | 23.0 | 21.2 | 20.8 |
| Standard deviation | 1.41 | 1.41 | 1.57 | 1.13 | 1.48 | 1.54 | 1.12 | 1.33 |

Table E4  Data for zeta potential of carbon black with varying C8 concentration and the initial calcium concentration 1000   (M.

| C8 Concentration (M) | 606.77 | 1213.54 | 2375.00 | 3588.54 | 7113.54 | 9411.46 |
| --- | --- | --- | --- | --- | --- | --- |
| (-) Zeta potential (mV) | 1 | 19.1 | 17.1 | 17.1 | 10.9 | 12.2 | 10.3 |
|  | 2 | 22.8 | 21.0 | 19.4 | 14.1 | 11.0 | 12.8 |
|  | 3 | 20.7 | 20.0 | 20.3 | 12.3 | 11.8 | 11.3 |
|  | 4 | 22.3 | 20.4 | 20.1 | 13.3 | 11.0 | 10.2 |
|  | 5 | 20.8 | 18.2 | 20.3 | 11.0 | 9.67 | 10.5 |
|  | 6 | 20.6 | 16.8 | 19.0 | 11.3 | 14.7 | 13.5 |
|  | 7 | 20.3 | 19.4 | 17.1 | 10.7 | 10.7 | 10.6 |
|  | 8 | 19.5 | 17.7 | 20.3 | 11.7 | 11.0 | 12.1 |
|  | 9 | 20.0 | 18.2 | 17.7 | 14.0 | 10.1 | 11.3 |
|  | 10 | 22.7 | 20.8 | 18.2 | 12.6 | 10.5 | 14.3 |
|  | 11 | 19.5 | 18.0 | 19.5 | 10.8 | 9.21 | 11.2 |
|  | 12 | 24.2 | 18.6 | 16.6 | 13.8 | 11.2 | 9.95 |
| Average zeta potential (mV) |  | 21.0 | 18.9 | 18.8 | 12.2 | 11.1 | 11.5 |
| Standard deviation | 1.53 | 1.37 | 1.34 | 1.26 | 1.35 | 1.34 |

Table E5  Data for zeta potential of carbon black with varying calcium concentration and the initial C8 concentration 0 (M.

| Calcium concentration (M) | 100 | 200 | 400 | 800 | 1000 | 2000 |
| --- | --- | --- | --- | --- | --- | --- |
| (-) Zeta potential (mV) | 1 | 29.0 | 24.6 | 20.0 | 15.7 | 14.2 | 14.7 |
|  | 2 | 29.4 | 26.1 | 19.5 | 15.4 | 12.6 | 13.6 |
|  | 3 | 26.2 | 27.1 | 17.8 | 16.2 | 15.9 | 14.0 |
|  | 4 | 27.0 | 24.8 | 16.0 | 14.5 | 16.8 | 14.2 |
|  | 5 | 27.2 | 25.4 | 18.8 | 15.4 | 14.3 | 12.9 |
|  | 6 | 26.3 | 25.9 | 19.6 | 14.7 | 16.1 | 13.5 |
|  | 7 | 27.3 | 24.6 | 20.1 | 16.6 | 15.4 | 12.2 |
|  | 8 | 29.2 | 24.0 | 20.3 | 17.4 | 16.8 | 14.3 |
|  | 9 | 26.2 | 26.7 | 16.9 | 14.4 | 14.3 | 12.5 |
|  | 10 | 26.8 | 25.1 | 18.0 | 15.9 | 15.7 | 14.7 |
|  | 11 | 28.7 | 24.6 | 20.1 | 16.0 | 12.2 | 15.9 |
|  | 12 | 26.1 | 24.4 | 17.6 | 14.2 | 14.4 | 12.5 |
| Average zeta potential (mV) |  | 27.5 | 25.3 | 18.7 | 15.5 | 14.9 | 13.8 |
| Standard deviation | 1.22 | 0.93 | 1.38 | 0.93 | 1.43 | 1.05 |

Table E6  Data for zeta potential of carbon black with varying calcium concentration and the initial C8 concentration 100 M.

| Calcium concentration (M) | 100 | 200 | 400 | 800 | 1000 | 2000 |
| --- | --- | --- | --- | --- | --- | --- |
| (-) Zeta potential (mV) | 1 | 27.4 | 22.1 | 20.5 | 13.3 | 14.2 | 14.9 |
|  | 2 | 27.3 | 19.4 | 19.1 | 13.6 | 16.9 | 13.6 |
|  | 3 | 25.3 | 20.2 | 18.1 | 16.6 | 15.6 | 14.0 |
|  | 4 | 25.1 | 21.0 | 20.0 | 13.4 | 15.1 | 12.9 |
|  | 5 | 25.4 | 22.9 | 20.3 | 15.6 | 14.2 | 10.5 |
|  | 6 | 24.3 | 22.2 | 17.7 | 16.4 | 14.6 | 10.7 |
|  | 7 | 24.2 | 22.7 | 21.0 | 12.4 | 14.4 | 10.9 |
|  | 8 | 27.4 | 19.0 | 19.1 | 16.7 | 15.0 | 12.5 |
|  | 9 | 23.3 | 19.1 | 20.8 | 14.8 | 16.1 | 13.4 |
|  | 10 | 25.8 | 22.0 | 20.0 | 15.9 | 14.1 | 13.6 |
|  | 11 | 23.9 | 20.2 | 19.2 | 14.8 | 12.4 | 11.9 |
|  | 12 | 23.3 | 22.0 | 18.0 | 14.2 | 15.6 | 12.0 |
| Average zeta potential (mV) |  | 25.2 | 21.1 | 19.5 | 14.8 | 14.9 | 12.6 |
| Standard deviation | 1.45 | 1.37 | 1.08 | 1.39 | 1.10 | 1.35 |

Table E7  Data for zeta potential of carbon black with varying calcium concentration and the initial C8 concentration 500 M.

| Calcium concentration (M) | 100 | 200 | 400 | 800 | 1000 | 2000 |
| --- | --- | --- | --- | --- | --- | --- |
| (-) Zeta potential (mV) | 1 | 22.9 | 20.0 | 21.0 | 18.0 | 14.7 | 13.8 |
|  | 2 | 25.4 | 24.3 | 19.3 | 14.9 | 14.7 | 12.4 |
|  | 3 | 21.3 | 22.1 | 21.2 | 15.4 | 15.9 | 11.1 |
|  | 4 | 24.8 | 22.4 | 18.2 | 15.8 | 11.1 | 11.6 |
|  | 5 | 25.4 | 22.0 | 19.7 | 19.7 | 15.0 | 11.3 |
|  | 6 | 26.2 | 23.9 | 17.5 | 18.6 | 14.2 | 13.7 |
|  | 7 | 25.3 | 20.9 | 17.3 | 14.0 | 14.4 | 12.8 |
|  | 8 | 25.2 | 24.8 | 20.5 | 18.7 | 13.9 | 11.4 |
|  | 9 | 25.9 | 22.5 | 17.7 | 15.7 | 14.8 | 14.5 |
|  | 10 | 24.1 | 21.2 | 22.0 | 15.9 | 15.0 | 13.0 |
|  | 11 | 23.7 | 24.1 | 20.2 | 16.4 | 15.1 | 14.1 |
|  | 12 | 24.4 | 19.9 | 20.9 | 15.9 | 14.3 | 12.6 |
| Average zeta potential (mV) |  | 24.6 | 22.3 | 19.6 | 16.6 | 14.4 | 12.7 |
| Standard deviation | 1.33 | 1.59 | 1.54 | 1.67 | 1.12 | 1.12 |

Table E8  Data for zeta potential of carbon black with varying calcium concentration and the initial C8 concentration 1000 M.

| Calcium concentration (M) |  | 100 | 200 | 400 | 800 | 1000 | 2000 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| (-) Zeta potential (mV) | 1 | 26.2 | 23.0 | 16.6 | 11.7 | 12.0 | 11.0 |
|  | 2 | 24.0 | 21.0 | 18.4 | 11.0 | 11.6 | 9.7 |
|  | 3 | 25.2 | 19.8 | 15.1 | 12.4 | 11.4 | 11.1 |
|  | 4 | 24.0 | 19.2 | 16.6 | 12.7 | 10.0 | 12.2 |
|  | 5 | 23.2 | 20.1 | 18.6 | 13.2 | 12.3 | 11.5 |
|  | 6 | 25.0 | 19.6 | 13.8 | 11.3 | 10.3 | 11.0 |
|  | 7 | 20.5 | 21.0 | 13.9 | 14.4 | 10.3 | 12.8 |
|  | 8 | 22.1 | 20.5 | 18.4 | 13.0 | 11.0 | 10.2 |
|  | 9 | 23.8 | 18.0 | 15.1 | 12.8 | 12.0 | 11.6 |
|  | 10 | 23.7 | 19.8 | 18.0 | 12.4 | 11.1 | 12.4 |
|  | 11 | 24.0 | 20.3 | 17.2 | 11.9 | 11.4 | 12.2 |
|  | 12 | 25.2 | 19.9 | 15.9 | 11.7 | 11.6 | 11.3 |
| Average zeta potential (mV) |  | 23.9 | 20.2 | 16.5 | 12.4 | 11.2 | 11.4 |
| Standard deviation | 1.45 | 1.15 | 1.65 | 0.90 | 0.71 | 0.87 |

## APPENDIX F

## Experimental data for zeta potential of paper fiber.

Weight of paper fiber		=  1.0 g

Volume of solution		=  40 ml

Temperature			=  30(C

pH				=  9

Table F1  Data for zeta potential of paper fiber with varying C8 concentration and without calcium addition.

| C8 Concentration (M) | 0.0 | 135.5 | 328.7 | 530.2 | 843.7 | 1071.9 | 2128.1 | 3127.1 | 4200.0 | 5156.3 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (-) Zeta potential (mV) | 1 | 31.0 | 26.0 | 26.7 | 22.0 | 22.3 | 20.5 | 21.3 | 20.7 | 20.6 | 21.9 |
|  | 2 | 28.9 | 27.8 | 28.0 | 21.1 | 19.4 | 21.6 | 20.4 | 20.1 | 19.1 | 19.6 |
|  | 3 | 33.2 | 28.1 | 27.1 | 24.5 | 19.7 | 19.8 | 20.3 | 19.6 | 20.3 | 20.1 |
|  | 4 | 30.1 | 26.4 | 24.6 | 19.4 | 20.2 | 19.4 | 20.5 | 20.9 | 20.7 | 19.8 |
|  | 5 | 29.1 | 26.0 | 26.7 | 21.3 | 19.0 | 17.7 | 19.1 | 21.9 | 20.5 | 20.8 |
|  | 6 | 29.5 | 29.1 | 28.1 | 21.4 | 20.4 | 19.2 | 18.1 | 22.1 | 19.2 | 21.5 |
|  | 7 | 30.8 | 27.8 | 27.2 | 24.0 | 19.3 | 17.7 | 20.6 | 20.7 | 18.6 | 21.4 |
|  | 8 | 30.2 | 27.2 | 27.9 | 20.9 | 20.8 | 18.8 | 19.5 | 18.7 | 19.7 | 19.3 |
|  | 9 | 31.2 | 28.9 | 24.8 | 20.8 | 18.7 | 19.0 | 17.8 | 19.8 | 19.0 | 20.9 |
|  | 10 | 28.9 | 27.4 | 27.6 | 22.8 | 18.9 | 21.4 | 17.5 | 20.1 | 19.4 | 19.9 |
|  | 11 | 30.4 | 27.2 | 25.5 | 20.7 | 20.2 | 17.1 | 17.2 | 21.9 | 20.8 | 20.9 |
|  | 12 | 31.1 | 27.7 | 24.7 | 21.6 | 19.0 | 17.7 | 18.5 | 19.1 | 20.9 | 19.1 |
| Average zeta potential (mV) |  | 30.4 | 27.5 | 25.0 | 21.7 | 19.8 | 19.2 | 19.2 | 20.5 | 19.9 | 20.4 |
| Standard deviation | 1.18 | 0.96 | 1.35 | 1.38 | 0.98 | 1.42 | 1.33 | 1.06 | 0.78 | 0.88 |

Table F2  Data for zeta potential of paper fiber with varying C8 concentration and the initial calcium concentration

500 M.

| C8 Concentration (M) | 0.00 | 100.03 | 209.90 | 410.31 | 623.75 | 844.90 | 1044.79 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| (-) Zeta potential (mV) | 1 | 21.2 | 15.8 | 13.3 | 10.8 | 10.7 | 11.2 | 11.7 |
|  | 2 | 17.1 | 17.2 | 12.0 | 10.5 | 10.0 | 8.2 | 10.4 |
|  | 3 | 18.0 | 15.4 | 13.3 | 10.3 | 10.8 | 11.6 | 12.5 |
|  | 4 | 18.4 | 16.4 | 12.5 | 10.9 | 10.0 | 11.7 | 8.3 |
|  | 5 | 19.3 | 14.7 | 9.7 | 10.6 | 10.6 | 10.5 | 11.0 |
|  | 6 | 17.7 | 17.7 | 9.7 | 10.4 | 12.1 | 9.6 | 8.7 |
|  | 7 | 18.5 | 15.6 | 12.0 | 9.9 | 10.0 | 8.9 | 7.7 |
|  | 8 | 18.6 | 14.7 | 11.2 | 9.4 | 10.8 | 8.4 | 8.8 |
|  | 9 | 20.6 | 15.8 | 10.2 | 10.8 | 9.4 | 11.5 | 8.8 |
|  | 10 | 20.0 | 16.9 | 9.6 | 13.9 | 10.9 | 10.6 | 8.9 |
|  | 11 | 18.8 | 14.7 | 9.5 | 11.3 | 10.3 | 9.9 | 9.4 |
|  | 12 | 19.2 | 15.6 | 10.0 | 11.7 | 12.1 | 9.4 | 9.4 |
| Average zeta potential (mV) |  | 19.0 | 15.9 | 11.1 | 10.9 | 10.6 | 10.1 | 9.6 |
| Standard deviation | 1.14 | 0.95 | 1.42 | 1.08 | 0.78 | 1.20 | 1.40 |

Table F3  Data for zeta potential of paper fiber with varying C8 concentration and the initial calcium concentration

1000 M.

| C8 Concentration (M) | 0.00 | 90.99 | 206.15 | 405.31 | 642.50 | 827.40 | 1054.17 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| (-) Zeta potential (mV) | 1 | 15.7 | 14.4 | 12.2 | 11.7 | 10.0 | 10.2 | 11.6 |
|  | 2 | 15.6 | 14.0 | 11.5 | 12.6 | 10.5 | 11.0 | 9.6 |
|  | 3 | 16.2 | 12.6 | 11.3 | 11.9 | 9.4 | 9.6 | 10.2 |
|  | 4 | 15.6 | 12.9 | 10.0 | 10.8 | 9.0 | 9.3 | 11.1 |
|  | 5 | 14.7 | 13.5 | 12.6 | 12.1 | 10.8 | 8.4 | 12.0 |
|  | 6 | 14.3 | 15.0 | 11.5 | 12.0 | 10.6 | 8.7 | 11.5 |
|  | 7 | 16.6 | 14.7 | 13.0 | 10.6 | 9.8 | 10.1 | 10.3 |
|  | 8 | 15.0 | 13.9 | 13.9 | 10.8 | 10.1 | 8.6 | 9.5 |
|  | 9 | 17.2 | 15.8 | 12.5 | 10.6 | 11.7 | 10.2 | 9.4 |
|  | 10 | 16.8 | 12.9 | 12.0 | 11.2 | 11.2 | 9.4 | 8.8 |
|  | 11 | 16.2 | 14.4 | 11.4 | 10.1 | 8.7 | 11.4 | 8.4 |
|  | 12 | 14.7 | 13.8 | 12.6 | 10.0 | 10.4 | 9.4 | 9.8 |
| Average zeta potential (mV) |  | 15.7 | 14.0 | 12.0 | 11.2 | 10.2 | 9.7 | 10.2 |
| Standard deviation | 0.88 | 0.90 | 0.96 | 0.81 | 0.86 | 0.89 | 1.11 |

Table F4  Data for zeta potential of paper fiber with varying calcium concentration and the initial C8 concentration

0 M.

| Calcium concentration (M) | 0.00 | 100.00 | 200.00 | 400.00 | 600.00 | 800.00 | 1000.00 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| (-) Zeta potential (mV) | 1 | 31.0 | 26.2 | 20.4 | 15.4 | 15.5 | 16.0 | 15.7 |
|  | 2 | 28.9 | 23.2 | 19.0 | 16.2 | 14.4 | 15.6 | 15.6 |
|  | 3 | 33.2 | 25.5 | 19.9 | 17.7 | 14.2 | 14.4 | 16.2 |
|  | 4 | 30.1 | 23.9 | 17.7 | 18.3 | 16.1 | 15.2 | 15.6 |
|  | 5 | 29.1 | 24.1 | 19.3 | 18.5 | 18.1 | 13.0 | 14.7 |
|  | 6 | 29.5 | 24.6 | 19.4 | 17.7 | 16.7 | 12.9 | 14.3 |
|  | 7 | 30.8 | 25.0 | 18.1 | 17.4 | 14.5 | 15.1 | 16.6 |
|  | 8 | 30.2 | 26.5 | 20.5 | 16.9 | 14.3 | 15.7 | 15.0 |
|  | 9 | 31.2 | 26.3 | 21.1 | 17.8 | 14.4 | 16.9 | 17.2 |
|  | 10 | 28.9 | 24.4 | 19.4 | 15.6 | 14.5 | 15.0 | 16.8 |
|  | 11 | 30.4 | 24.6 | 20.0 | 15.4 | 15.3 | 15.1 | 16.2 |
|  | 12 | 31.1 | 23.9 | 19.5 | 16.7 | 16.3 | 16.3 | 14.7 |
| Average zeta potential (mV) |  | 30.4 | 24.9 | 19.5 | 17.0 | 15.4 | 15.1 | 15.7 |
| Standard deviation | 1.18 | 1.02 | 0.93 | 1.06 | 1.17 | 1.15 | 0.88 |

Table F5  Data for zeta potential of paper fiber with varying calcium concentration and the initial C8 concentration

500 M.

| Calcium concentration (M) | 0 | 100 | 200 | 400 | 600 | 800 | 1000 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| (-) Zeta potential (mV) | 1 | 23.7 | 17.0 | 18.1 | 14.5 | 8.9 | 9.2 | 9.5 |
|  | 2 | 24.0 | 17.2 | 16.4 | 12.5 | 8.8 | 10.7 | 10.0 |
|  | 3 | 20.8 | 16.3 | 16.5 | 13.2 | 9.7 | 8.4 | 9.3 |
|  | 4 | 23.0 | 18.5 | 17.4 | 12.0 | 10.2 | 8.9 | 9.6 |
|  | 5 | 22.9 | 16.7 | 17.9 | 13.2 | 8.8 | 10.5 | 9.5 |
|  | 6 | 23.1 | 15.0 | 15.0 | 13.1 | 9.9 | 9.8 | 7.7 |
|  | 7 | 21.0 | 17.4 | 16.6 | 11.5 | 8.2 | 8.9 | 8.4 |
|  | 8 | 22.5 | 18.5 | 15.7 | 11.3 | 10.0 | 9.6 | 7.5 |
|  | 9 | 22.2 | 17.2 | 13.9 | 14.5 | 8.8 | 8.5 | 9.1 |
|  | 10 | 23.1 | 17.4 | 13.5 | 12.3 | 9.5 | 10.5 | 8.0 |
|  | 11 | 21.2 | 16.7 | 14.9 | 13.1 | 10.4 | 11.0 | 11.2 |
|  | 12 | 20.4 | 18.3 | 16.0 | 12.4 | 10.1 | 10.2 | 9.3 |
| Average zeta potential (mV) |  | 22.3 | 17.2 | 16.0 | 12.8 | 9.4 | 9.7 | 9.1 |
| Standard deviation | 1.15 | 0.95 | 1.41 | 0.97 | 0.67 | 0.86 | 1.00 |

Table F6  Data for zeta potential of paper fiber with varying calcium concentration and the initial C8 concentration

1000 M.

| Calcium concentration (M) | 0 | 100 | 200 | 400 | 600 | 800 |
| --- | --- | --- | --- | --- | --- | --- |
| (-) Zeta potential (mV) | 1 | 20.2 | 14.2 | 11.6 | 8.5 | 9.4 | 8.0 |
|  | 2 | 18.5 | 13.0 | 12.4 | 9.1 | 8.8 | 9.8 |
|  | 3 | 19.3 | 14.3 | 9.9 | 10.7 | 10.2 | 8.3 |
|  | 4 | 19.0 | 15.8 | 11.5 | 9.4 | 11.2 | 7.8 |
|  | 5 | 20.1 | 14.5 | 10.7 | 9.8 | 9.6 | 10.8 |
|  | 6 | 21.1 | 16.0 | 10.0 | 11.7 | 8.9 | 8.8 |
|  | 7 | 20.6 | 13.1 | 11.7 | 9.8 | 8.9 | 7.6 |
|  | 8 | 20.2 | 14.2 | 10.0 | 10.2 | 9.8 | 8.2 |
|  | 9 | 21.2 | 13.8 | 9.6 | 11.6 | 10.0 | 9.7 |
|  | 10 | 18.9 | 14.5 | 10.2 | 11.7 | 11.3 | 9.7 |
|  | 11 | 21.5 | 14.8 | 10.6 | 11.5 | 11.5 | 9.6 |
|  | 12 | 17.9 | 13.2 | 11.2 | 12.8 | 10.2 | 8.9 |
| Average zeta potential (mV) |  | 19.9 | 14.3 | 10.8 | 10.6 | 10.0 | 8.9 |
| Standard deviation | 1.10 | 0.92 | 0.84 | 1.24 | 0.92 | 0.95 |

CURRICULUM VITAE

Name : 	Miss Sureerat Jairakdee

Birth date : 	March 7, 1978

Nationality :	Thai

University education :

  - Bachelor of Engineering (Chemical Engineering)

Department of Chemical Engineering,

Faculty of Engineering,

King Mongkut’s University of Technology Thonburi, Bangkok , Thailand